# Material Compatibility with Gas C = Compatible Material NC = Non-Compatible Material

## Gas - Material Compatibility - Compatibility with Metals.

Gas; Aluminum; Brass; Copper; Monel; Stainless Steel. ACETYLENE; C; C; NC; C; C. AIR; C; C; C; C; C. AMMONIA; C; NC; NC; C; C. ARGON; -; C; C; C; C. 1,3 - BUTADIENE; -; -; -; -; -. 2 - BUTENE; -; -; -; -; -. N - BUTANE; C; C; C; C; C. CARBON DIOXIDE; C; C; C; C; C. CARBON MONOXIDE; C; C; C; C; C. CHLORINE; NC; NC; NC; C; C. ETHANE; C; C; C; C; C. ETHYL CHLORIDE; C; C; C; C; C. ETHYLENE; C; C; C; C; C. ETHYLENE OXIDE; -; -; -; -; -. HALOCARBON-14; -; -; -; -; -. HALOCARBON-22; C; C; C; C; C. HALOCARBON-23; C; C; C; C; C. HALOCARBON-116; C; C; C; C; C. HALOCARBON-134A; -; -; -; -; -. HALOCARBON-218; -; -; -; -; -. HELIUM; C; C; C; C; C. HYDROGEN; C; C; C; C; C. HYDROGEN BROMIDE; NC; NC; NC; C; C. HYDROGEN CHLORIDE; NC; NC; NC; C; C. HYDROGEN SUFIDE; C; C; -; C; C. ISOBUTANE; C; C; C; C; C. ISOBUTYLENE; C; C; C; C; C. METHANE; C; C; C; C; C. METHYL CHLORIDE; NC; C; C; C; C. NEON; C; C; C; C; C. NITRIC OXIDE; -; -; -; -; -. NITROGEN; C; C; C; C; C. NITROGEN DIOXIDE; C; NC; NC; NC; C. OXYGEN; NC; C; C; C; -. PROPANE; C; C; C; C; C. PROPYLENE; C; C; C; C; C. SUFUR DIOXIDE; C; NC; C; C; C. SUFUR HEXAFLUORIDE; C; C; C; C; C. XENON; C; C; C; C; C.

Top Next.

## Gas - Material Compatibility - Compatibility with Plastics.

Gas; Kel—F; Teflon; Tefzel; Kymar. ACETYLENE; C; C; C; C. AIR; C; C; C; C. AMMONIA; C; C; C; NC. ARGON; C; C; C; C. 1,3 - BUTADIENE; -; -; -; -. 2 - BUTENE; -; -; -; -. N - BUTANE; C; C; C; C. CARBON DIOXIDE; C; C; C; C. CARBON MONOXIDE; C; C; C; C. CHLORINE; C; C; C; C. ETHANE; C; C; C; C. ETHYL CHLORIDE; C; C; C; C. ETHYLENE; C; C; C; C. ETHYLENE OXIDE; -; -; -; -. HALOCARBON-14; -; -; -; -. HALOCARBON-22; C; C; C; C. HALOCARBON-23; C; C; C; C. HALOCARBON-116; C; C; C; C. HALOCARBON-134A; -; -; -; -. HALOCARBON-218; -; -; -; -. HELIUM; C; C; C; C. HYDROGEN; C; C; C; C. HYDROGEN BROMIDE; C; C; C; C. HYDROGEN CHLORIDE; C; C; C; C. HYDROGEN SUFIDE; C; C; C; C. ISOBUTANE; C; C; C; C. ISOBUTYLENE; C; C; C; C. METHANE; C; C; C; C. METHYL CHLORIDE; C; C; C; C. NEON; C; C; C; C. NITRIC OXIDE; -; -; -; -. NITROGEN; C; C; C; C. NITROGEN DIOXIDE; C; C; -; -. OXYGEN; C; C; C; C. PROPANE; C; C; C; C. PROPYLENE; C; C; C; C. SUFUR DIOXIDE; C; C; C; C. SUFUR HEXAFLUORIDE; C; C; C; C. XENON; C; C; C; C.

Top Next.

## Gas - Material Compatibility - Compatibility with Elastomers.

Gas; Viton; Buna—N; Neoprene. ACETYLENE; C; C; C. AIR; C; C; C. AMMONIA; NC; C; C. ARGON; C; C; C. 1,3 - BUTADIENE; -; -; -. 2 - BUTENE; -; -; -. N - BUTANE; C; C; C. CARBON DIOXIDE; C; -; -. CARBON MONOXIDE; C; C; C. CHLORINE; C; NC; NC. ETHANE; C; C; C. ETHYL CHLORIDE; C; C; C. ETHYLENE; C; C; C. ETHYLENE OXIDE; -; -; -. HALOCARBON-14; -; -; -. HALOCARBON-22; C; C; C. HALOCARBON-23; C; C; C. HALOCARBON-116; C; C; C. HALOCARBON-134A; -; -; -. HALOCARBON-218; -; -; -. HELIUM; C; C; C. HYDROGEN; C; C; C. HYDROGEN BROMIDE; C; NC; NC. HYDROGEN CHLORIDE; C; NC; NC. HYDROGEN SUFIDE; NC; C; C. ISOBUTANE; C; C; C. ISOBUTYLENE; C; C; C. METHANE; C; C; C. METHYL CHLORIDE; C; NC; NC. NEON; C; C; C. NITRIC OXIDE; -; -; -. NITROGEN; C; C; C. NITROGEN DIOXIDE; NC; NC; NC. OXYGEN; -; NC; NC. PROPANE; C; C; C. PROPYLENE; C; C; NC. SUFUR DIOXIDE; C; NC; NC. SUFUR HEXAFLUORIDE; C; C; C. XENON; C; C; C.

Top.